## Slide 1
Chart: Wavelength (nm)
| 200 | 210 | 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300 | 310 | 320 | 330 | 340 | 350 | 360 | 370 | 380 | 390 | 400 | 410 | 420 | 430 | 440 | 450 | 460 | 470 | 480 | 490 | 500 | 510 | 520 | 530 | 540 | 550 | 560 | 570 | 580 | 590 | 600 | 610 | 620 | 630 | 640 | 650 | 660
GEMCITABINE (GEM) | 1.1153 | 0.6027 | 0.3558 | 0.2618 | 0.2834 | 0.4294 | 0.5658 | 0.5108 | 0.243 | 0.179 | 0.0967 | 0.0686 | 0.0655 | 0.0638 | 0.0612 | 0.06 | 0.059 | 0.0574 | 0.0563 | 0.055 | 0.0542 | 0.0532 | 0.0525 | 0.0518 | 0.0501 | 0.0509 | 0.0503 | 0.05 | 0.049 | 0.0489 | 0.0487 | 0.0481 | 0.0479 | 0.0476 | 0.0468 | 0.047 | 0.0467 | 0.0465 | 0.0455 | 0.0453 | 0.0463 | 0.0464 | 0.0458 | 0.0456 | 0.0448 | 0.0454 | 0.0457
B
SM2: (A) Drug stability in CPVA-p4GEMC conjugate determined by UV spectrophotometry. The conjugate was incubated at pH 1, and low-Mw products released from dialysis tube were analyzed by UV absorbance every 24h. UV spectra of N-isobutyryl Gemcitabine (a), CPVA-p4GEMC conjugate (b) and the products of conjugate hydrolysis after 48 and 24 h incubation (c-d) are shown (λmax 268 nm). (B) UV absorbance of Gemcitabine at pH 1, (λmax 260 nm).
Chart: Wavelength (nm)
| 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300 | 310 | 320 | 330 | 340 | 350 | 360 | 370 | 380 | 390 | 400
GEMC | 0.8932 | 0.608 | 0.4174 | 0.4226 | 0.5036 | 0.6006 | 0.5658 | 0.3669 | 0.2576 | 0.2181 | 0.1479 | 0.1071 | 0.0923 | 0.0893 | 0.0868 | 0.0838 | 0.0818 | 0.0793 | 0.0777
CPVA-p4GEMC | 0.7443 | 0.5084 | 0.3542 | 0.3565 | 0.4174 | 0.4911 | 0.464 | 0.31 | 0.224 | 0.1919 | 0.1341 | 0.1004 | 0.0879 | 0.0852 | 0.0831 | 0.0803 | 0.0785 | 0.0763 | 0.0747
CPVA-p4GEMC, pH1, 48h | 0.3766 | 0.2726 | 0.2046 | 0.2023 | 0.219 | 0.2409 | 0.2289 | 0.1717 | 0.1395 | 0.1251 | 0.1002 | 0.0854 | 0.0788 | 0.0769 | 0.0756 | 0.0734 | 0.0721 | 0.0702 | 0.0689
CPVA-p4GEMC, pH1, 24h | 0.2868 | 0.1947 | 0.1343 | 0.1415 | 0.1734 | 0.2035 | 0.1868 | 0.1151 | 0.0762 | 0.0667 | 0.0633 | 0.0606 | 0.0575 | 0.0564 | 0.0556 | 0.0541 | 0.0532 | 0.0519 | 0.0511
a