## Slide 1
Supplement figures

## Slide 2
5 mm
0.5 mm W line
b
10 mm
2 mm W line
c
20 mm
10 mm W line
d
2 mm
blanket W film
a
Figure S1. SEM micrograph reveal cross-sectional images of blanket tungsten film and comb structures.
silicon substrate
silicon substrate
silicon substrate
silicon substrate
Notes: X-section_tilt076

## Slide 3
Figure S2. SEM micrographs reveal cell morphology on (a) polished tungsten and (b) polished silicon oxide surface.
50 mm
60 mm
a
b
20 mm
30 mm
tungsten
tungsten
silicon oxide
silicon oxide

## Slide 4
4.30 hours
10 mm
2.25 hours
0.5 hours
1.25 hours
6.0 hours
8.25 hours
12.20 hours
26.0 hours
49.25 hours
36.2 hours
10 mm
10 mm
10 mm
10 mm
10 mm
10 mm
10 mm
10 mm
10 mm
Figure S3. SEM micrographs (70o tilted) of Vero cells on 10 mm comb structures with incubation time from 0.5 to 49.25 hours.

## Slide 5
0.18 mm comb
a
b
c
d
e
0.25 mm comb
50 mm comb
2 mm comb
10 mm W/ 90 mm SiO2
Figure S4. Fluorescence confocal micrographs reveal adherent cells on comb structures with line widths of (a) 0.18 mm, (b) 0.25 mm, (c) 2 mm, (d) 50 mm, and (e) line structures with 10 mm tungsten and 90 mm silicon dioxide. Scale bars represent 50 mm.
50 mm
Notes: C:\tttsui\Veero AP WCMP\2016_6_16_Veero_cells_Megan_24hrs_batch3_IC_0.18x0.18_random\tif

## Slide 6
50 mm
50 mm
a
b
c
d
Figure S5. Example cell geometries used for the modeling . They were selected from actual cells adhered on (a) field tungsten area, (b) bare silicon,(c) 2 mm, and (d) 0.18 mm wide isolated tungsten lines.
20 mm
bare silicon
20 mm
field W
2 mm isolated line
0.18 mm isolated line

## Slide 7
200 mm
200 mm
200 mm
200 mm
500 mm
500 mm
before-rework
after-rework
10mm W-90mm SiO2
10mm W-10mm SiO2
0.18mm W-0.18mm SiO2
a
b
c
Figure S6. Examples of comb structures before and after mechanical scrubbing rework process: a) 10 mm tungsten-90 mm silicon dioxide; (b) 10 mm tungsten-10 mm silicon dioxide; (c) 0.18 mm tungsten-0.18 mm silicon dioxide.