## Slide 1
Waffle method for cryo-FIB/SEM sample preparation
Developed by Kotaro Kelley

## Slide 2
Waffle method for cryo-FIB/SEM sample preparation
Developed by Kotaro Kelley

## Slide 4
Step 0
Prepare hardware for waffling

## Slide 5
Step 0

## Slide 6
Step 0
a) Polish planchette hats

## Slide 7
Step 0
a) Polish planchette hats

## Slide 8
Step 0
a) Polish planchette hats
polish

## Slide 9
b) Coat with 1-hexadecene
Step 0
a) Polish planchette hats
polish

## Slide 10
b) Coat with 1-hexadecene
Step 0
a) Polish planchette hats

## Slide 11
b) Coat with 1-hexadecene
Step 0
a) Polish planchette hats

## Slide 12
b) Coat with 1-hexadecene
Step 0
a) Polish planchette hats

## Slide 13
b) Coat with 1-hexadecene
Step 0
a) Polish planchette hats

## Slide 14
b) Coat with 1-hexadecene
Step 0
a) Polish planchette hats

## Slide 15
b) Coat with 1-hexadecene
Step 0
a) Polish planchette hats

## Slide 16
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0

## Slide 17
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0
c) Sputter ~25nm carbon coat on non-grid bar side

## Slide 18
c) Sputter ~25nm carbon coat on non-grid bar side
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0

## Slide 19
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0
c) Sputter ~25nm carbon coat on non-grid bar side

## Slide 20
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0
d) Clean HPF tip with ethanol
c) Sputter ~25nm carbon coat on non-grid bar side

## Slide 21
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0
d) Clean HPF tip with ethanol
c) Sputter ~25nm carbon coat on non-grid bar side

## Slide 22
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0
d) Clean HPF tip with ethanol
c) Sputter ~25nm carbon coat on non-grid bar side

## Slide 23
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0
d) Clean HPF tip with ethanol
c) Sputter ~25nm carbon coat on non-grid bar side

## Slide 24
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0
d) Clean HPF tip with ethanol
e) Glow discharge/plasma clean grid
c) Sputter ~25nm carbon coat on non-grid bar side

## Slide 25
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0
d) Clean HPF tip with ethanol
e) Glow discharge/plasma clean grid
c) Sputter ~25nm carbon coat on non-grid bar side

## Slide 26
b) Coat with 1-hexadecene
a) Polish planchette hats
Step 0
d) Clean HPF tip with ethanol
e) Glow discharge/plasma clean grid
c) Sputter ~25nm carbon coat on non-grid bar side

## Slide 27
Step 1

## Slide 28
Step 1
Prepare sample for waffling

## Slide 29
Step 1

## Slide 30
Step 1
Assemble bottom portion of waffle

## Slide 31
Step 1
Assemble bottom portion of waffle
*may be assembled inside or outside of the HPF tip

## Slide 32
Step 1
Assemble bottom portion of waffle
*may be assembled inside or outside of the HPF tip

## Slide 33
Step 1
Assemble bottom portion of waffle
*may be assembled inside or outside of the HPF tip

## Slide 34
Step 1
Assemble bottom portion of waffle
*may be assembled inside or outside of the HPF tip

## Slide 35
Step 1
Assemble bottom portion of waffle
*may be assembled inside or outside of the HPF tip

## Slide 36
Step 1
*may be assembled inside or outside of the HPF tip
Assemble bottom portion of waffle

## Slide 37
Step 1
*may be assembled inside or outside of the HPF tip
Apply sample to waffle mold

## Slide 38
Step 1
*may be assembled inside or outside of the HPF tip
Apply sample to waffle mold
Sample

## Slide 39
Step 1
*may be assembled inside or outside of the HPF tip
Apply sample to waffle mold

## Slide 40
Step 1
*may be assembled inside or outside of the HPF tip
Apply sample to waffle mold

## Slide 41
Step 1
*may be assembled inside or outside of the HPF tip
Cover waffle with top planchette

## Slide 42
Step 1
Enclose planchettes in HPF tip

## Slide 43
Step 1
Enclose planchettes in HPF tip

## Slide 44
Step 1
Enclose planchettes in HPF tip

## Slide 45
Step 1
Enclose planchettes in HPF tip

## Slide 46
Step 1
Enclose planchettes in HPF tip

## Slide 47
Step 1
Enclose planchettes in HPF tip

## Slide 48
Step 1
Enclose planchettes in HPF tip

## Slide 49
Step 1
Enclose planchettes in HPF tip

## Slide 50
Step 1
HPF sample

## Slide 51
Step 1
HPF sample
BANG!
in HPF

## Slide 52
Step 1
HPF sample
BANG!
in HPF

## Slide 53
Step 1
Disassemble HPF tip
in LN2

## Slide 54
Step 1
Disassemble HPF tip
in LN2

## Slide 55
Step 1
Disassemble HPF tip
in LN2

## Slide 56
Step 1
Disassemble HPF tip
in LN2

## Slide 57
Step 1
Disassemble planchettes
in LN2

## Slide 58
Step 1
Disassemble planchettes
in LN2

## Slide 59
Step 1
Disassemble planchettes
in LN2

## Slide 60
Step 1
Remove spacer
in LN2

## Slide 61
Step 1
Remove spacer
in LN2

## Slide 62
Step 1
Remove spacer
in LN2

## Slide 63
Step 1
in LN2

## Slide 64
Step 1
Clip grid carefully
in LN2 or LN2 gas

## Slide 65
Step 1
Clip grid carefully
in LN2 or LN2 gas

## Slide 66
Step 1
Clip grid carefully
in LN2 or LN2 gas

## Slide 67
Step 1
(optional) Sputter ~5nm of platinum onto grid
in cold chamber

## Slide 68
Step 1
(optional) Sputter ~5nm of platinum onto grid
in cold chamber

## Slide 69
Step 1
(optional) Sputter ~5nm of platinum onto grid
in cold chamber

## Slide 70
Step 1
(optional) Screen waffle in cryo-CLEM
on cold stage

## Slide 71
Step 1
(optional) Screen waffle in cryo-CLEM
on cold stage

## Slide 72
Step 1
(optional) Screen waffle in cryo-CLEM
on cold stage

## Slide 73
Step 1
(optional) Screen waffle in cryo-CLEM
on cold stage

## Slide 74
Step 1
(optional) Screen waffle in cryo-CLEM
on cold stage

## Slide 75
Step 1
The waffle is ready for milling!
store in clean LN2 and separate dewar

## Slide 76
Step 1
The waffle is ready for milling!
store in clean LN2 and separate dewar
Example

## Slide 77
Step 1
The waffle is ready for milling!
store in clean LN2 and separate dewar
Example

## Slide 78
Step 2

## Slide 79
Step 2
Mill the waffle

## Slide 80
Step 2
Place waffle grid into un-tilted stage (orient grid squares to be parallel with the holder)
in LN2 or LN2 gas

## Slide 81
Step 2
Place waffle grid into un-tilted stage (orient grid squares to be parallel with the holder)
in LN2 or LN2 gas

## Slide 82
Step 2
Place waffle grid into un-tilted stage (orient grid squares to be parallel with the holder)
in LN2 or LN2 gas

## Slide 83
Step 2
Insert stage into cryo-FIB/SEM
in cold chamber

## Slide 84
Step 2
Insert stage into cryo-FIB/SEM
in cold chamber

## Slide 85
Step 2
Apply 1-4 microns of GIS platinum
in cold chamber

## Slide 86
Step 2
Apply 1-4 microns of GIS platinum
in cold chamber

## Slide 87
Step 2
Apply 1-4 microns of GIS platinum
in cold chamber

## Slide 88
Step 2
Apply 1-4 microns of GIS platinum
in cold chamber

## Slide 89
Step 2
Apply 1-4 microns of GIS platinum
in cold chamber

## Slide 90
Step 2
Draw grid bar lines with FIB
in cold chamber

## Slide 91
Step 2
Draw grid bar lines with FIB
in cold chamber

## Slide 92
Step 2
Draw grid bar lines with FIB
in cold chamber

## Slide 93
Step 2
Draw grid bar lines with FIB
in cold chamber

## Slide 94
Step 2
in cold chamber
Draw grid bar lines with FIB

## Slide 95
Step 2
in cold chamber
Example
Draw grid bar lines with FIB

## Slide 96
Step 2
in cold chamber
Example
Draw grid bar lines with FIB

## Slide 97
Step 2
FIB-mill trenches: 2 trenches per area of interest (in flat holder)
in cold chamber

## Slide 98
Step 2
FIB-mill trenches: 2 trenches per area of interest (in flat holder)
in cold chamber

## Slide 99
Step 2
FIB-mill trenches: 2 trenches per area of interest (in flat holder)
in cold chamber

## Slide 100
Step 2
FIB-mill trenches: 2 trenches per area of interest (in flat holder)
in cold chamber

## Slide 101
Step 2
FIB-mill trenches: 2 trenches per area of interest (in flat holder)
in cold chamber

## Slide 102
Step 2
FIB-mill trenches: 2 trenches per area of interest (in flat holder)
in cold chamber

## Slide 103
Step 2
FIB-mill trenches: 2 trenches per area of interest (in flat holder)
in cold chamber
Example
(2 pairs of trenches for higher throughput shown)

## Slide 104
Step 2
FIB-mill trenches: 2 trenches per area of interest (in flat holder)
in cold chamber
Example
(2 pairs of trenches for higher throughput shown)

## Slide 105
Step 2
in cold chamber
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)

## Slide 106
Step 2
in cold chamber
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)

## Slide 107
Step 2
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)
in cold chamber

## Slide 108
Step 2
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)
in cold chamber

## Slide 109
Step 2
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)
in cold chamber

## Slide 110
Step 2
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)
Example
in cold chamber

## Slide 111
Step 2
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)
Example
in cold chamber

## Slide 112
Step 2
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)
Example
in cold chamber
Recommended: FIB-mill a stress-relief notch

## Slide 113
Step 2
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)
Example
in cold chamber
Recommended: FIB-mill a stress-relief notch

## Slide 114
Step 2
FIB-mill lamellae: Always mill on leading Pt edge (in tilted holder)
Example
in cold chamber
Recommended: FIB-mill a stress-relief notch

## Slide 115
Step 2
FIB-mill all lamellae in parallel
in cold chamber

## Slide 116
Step 2
FIB-mill all lamellae in parallel
in cold chamber

## Slide 117
Step 2
FIB-mill all lamellae in parallel
in cold chamber

## Slide 118
Step 2
FIB-mill all lamellae in parallel
in cold chamber
Example

## Slide 119
Step 2
FIB-mill all lamellae in parallel
in cold chamber
Example

## Slide 120
Finished!
Waffle lamellae are ready for cryoET
store in clean LN2 and separate dewar

## Slide 121
Finished!
Waffle lamellae are ready for cryoET
store in clean LN2 and separate dewar